CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter Product code: FCH711

Production date: Feb. 11, 2020 ~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCH711 | Sky Blue | 25μm | ✘ | 160~170℃ | 3.5 | Hexagon | 0.08~3mm | ✔ | - | - | 7.8 | ✔ |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polyethylene terephthalate | 25038-59-9 | 607-507-1 | 97.89 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 1.8 |
| Aluminum | 7429-90-5 | 231-072-3 | 0.01 |
| FD&C Blue 1 (CI.42090) | 3844-45-9 | 223-339-8 | 0.24 |
| FD&C Yellow 5(CI.19140) | 1934-21-0 | 217-699-5 | 0.06 |

SECTION 4. TEST REPORT ON HEAVY METALS