CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Glitter

Product code: FCH406A	batch number:20190216-A03 Production date: Feb. 11, 2020 ~ Feb.18, 2020

Expiry date: Feb. 18, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCH406A | Light Brown | 25μm | ✔ | 170~190℃ | 6.5 | Hexagon | 0.08~3mm | - | - | ✔ | 7~7.5 | ✘ |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polyethylene terephthalate | 25038-59-9 | 607-507-1 | 95.71 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 2.6 |
| Aluminum | 7429-90-5 | 231-072-3 | 0.01 |
| FD&C Red 40 (C.I.16035) | 25956-17-6 | 247-368-0 | 0.66 |
| FD&C Yellow 5 (C.I.19140) | 1934-21-0 | 217-699-5 | 0.64 |
| Carbon Black (C.I. 77266) | 1333-86-4 | 215-609-9 | 0.38 |

SECTION 4. TEST REPORT ON HEAVY METALS