SPECIFICATION

Coloron Pigment

(Code:SW080AY)

| Assay | Spec. Values | Test Method |
| --- | --- | --- |
| Synthetic Fluorphlogopite | 85.0-96.0% | CRTM-51 |
| TiO2 | 4.0-14.0% | CRTM-48 |
| SnO2 | ≤1.0% | CRTM-48 |
| Particle Size | 50-250 µm | CRTM-42 |
| PH Value | 6.0-10.0 | CRTM-45 |
| Density: | 2.3-3.2g/cm3 | CRTM-47 |
| Oil absorption | 60-150g/100g | CRTM-46 |

Zhongshan Zhongtai Pigment Co.,Ltd

Website: http://www.zsztyl.com	E-mail: zhongtaiyanliao@163.com